Zirconium – Cerium and Zirconium – Lanthanum complexed polyvinyl alcohol films for efficient fluoride removal from aqueous solution

Supplementary Material

Table of contents							Page No.

- Synthetic Scheme                                                                                          2

- EDS mapping of ZLPC with fluoride                                                           2

- EDS mapping of ZCPC with fluoride                                                           3

- EDS of different parts of the film						3-4

- Table on Chemical Stability                                                                           4

- Table of Swelling Index                                                                       	4

- Table of IR peaks of the films							4-5

- Kinetics of adsorption 							5

- Adsorption isotherm								5-6

- Computational data                                                                                        6

- Real time water sample analysis                        				7

- Synthetic scheme

Scheme 1 Synthesis of MPC films  used for defluoridation

2. EDS mapping of ZLPC with fluoride

Figure 1 Distribution pattern of the metal ions and adsorbed fluoride in ZLPC

3.  EDS mapping of ZCPC with fluoride

Figure 2  Distribution pattern of the metal ions and adsorbed fluoride in ZCPC

4. The EDS analysis for different parts of the same film and the value of relative

weight percentage of different metal ions

Table 1: Relative weight percentage of different ions in ZLPC in EDS

| Metal ion | Weight Percentage |  |  | Average weight percentage |
| --- | --- | --- | --- | --- |
|  | Part 1 | Part 2 | Part 3 |  |
| Zr4+ | 6.86 | 6.15 | 5.88 | 6.30 |
| La3+ | 0.67 | 0.15 | 0.51 | 0.44 |

Table 2: Relative weight percentage of different ions in ZCPC in EDS

| Metal ion | Weight Percentage |  |  | Average weight percentage |
| --- | --- | --- | --- | --- |
|  | Part 1 | Part 2 | Part 3 |  |
| Zr4+ | 5.62 | 5.97 | 5.37 | 5.65 |
| Ce4+ | 4.08 | 4.21 | 3.4 | 3.90 |

5.Chemical stability

Table 3: Chemical stability of the polymer films in acidic and basic medium

| Polymer Films | % Weight loss |  |
| --- | --- | --- |
|  | 0.1 mol/L HCl | 0.1mol/L NaOH |
| ZLPC | 4.0 | 1.5 |
| ZCPC | 4.2 | 1.6 |

6. Swelling index

Table 4: Swelling index of the polymer films

| Polymer films | Swelling Index |
| --- | --- |
| ZLPC | 3.49 |
| ZCPC | 3.61 |
| PVA | 6.39 |

7. Shifts in the IR peaks

Table 5: Vibrational frequencies of frequency of functional groups in IR spectra

| Functional group | Peak position in PVA (cm−1) | Peak position in ZLPC (cm−1) | Peak position in ZCPC (cm−1) |
| --- | --- | --- | --- |
| O−Hstr,, | 3363 | 3434 | 3434 |
| C=Ostr | 1718 | 1628 | 1628 |
| in plane C−Hdef | 1425 | 1463 | 1447 |
| C−Ostr | 1083 | 1018 | 1023 |
| out of plane O−Hdef | 850 and 649 | 795 and 605 | 795 and 580 |

8. Kinetics of adsorption

Table 6: Percentage fluoride removal with time

| Time (min) | 5 | 10 | 15 | 20 | 25 | 30 | 45 | 60 | 120 | 180 | 240 | 300 | 360 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| % F- removal by ZLPC | 30 | 44 | 56 | 66 | 71 | 78 | 85 | 94 | 94 | 94 | 95 | 95 | 95 |
| % F- removal by ZCPC | 46 | 64 | 76 | 79 | 86 | 89 | 93 | 95 | 96 | 96 | 97 | 97 | 97 |

Table 7: Determination of the best fit of kinetic data into pseudo second order kinetic model

| Polymer films | T (K) | qe,cal (mg/g) | qe,exp (mg/g) | Chi square | RMSE |
| --- | --- | --- | --- | --- | --- |
| ZLPC | 303 | 8.51 | 8.35 | 0.02618 | 0.0398 |
|  | 313 | 1.54 | 1.78 |  |  |
|  | 323 | 1.51 | 1.75 |  |  |
| ZCPC | 303 | 8.21 | 8.07 | 0.0052 | 0.0429 |
|  | 313 | 2.17 | 2.25 |  |  |
|  | 323 | 1.58 | 1.71 |  |  |

9. Graphs of Adsorption isotherms

Figure 3Linear fit of Freundlich Adsorption Isotherm a) ZLPC and  b) ZCPC

Figure 4

Non Linear fit of Langmuir adsorption isotherm a) ZLPC and b) ZCPC

Non Linear fit of Freundlich adsorption isotherm c) ZLPC and d) ZCPC

10. Computational data

Table 8: The energetics for the DFT optimized molecules proposed in the mechanistic adsorption of fluoride by the metal loaded polymer.

| Species | Energy (au) |
| --- | --- |
| [Zr(PVA-5-)2(H2O)2] | −1508.42 |
| Fluoride | −99.83 |
| Water | −76.41 |
| [Zr(PVA-5-)2(F)2] | −1555.77 |

The ΔGf’ calculated in kJ/mol is −330.05 kJ/mol

11.   Real time water analysis

Table 9: Water profile of the treated groundwater

| Water Quality Parameter | Borewell water | ZLPC treated water | ZCPC treated water |
| --- | --- | --- | --- |
| pH | 8.05 | 7.26 | 7.19 |
| Conductivity mS/cm | 0.065 | 0.074 | 0.070 |
| TDS (ppm) | 1110 | 1090 | 1060 |
| Hardness (grains per gallon) | 49.7 | 21.34 | 19.25 |
| Fluoride | 2.12 | 0.682 | 0.676 |