Figure S1. X-ray diffraction patterns of TiO2 powders: Sample 1 = NPs (blue line) and Sample 2 = FPs (red lines).  The crystalline phase of both samples is anatase as characterized by the strong diffraction peaks at 25° and 48°. The diffraction peaks of sample 2 are sharper and bigger than those of sample 1. Analysis of particle size using the Scherrer equation reveals that sample 2 has a higher crystallite size than sample 1 (dXRD for sample 2 = 59 nm; dXRD for sample 1 = 15 nm).

TiO2 – NPs					TiO2 – FPs

Figure S2.  SEM images of the two TiO2 powder samples used in this study, which show that the particles tended to form relatively large aggregates.  The scale bar in each micrograph is 10 m.

Figure S3.  Impact of GIT region on the microstructure of TiO2 particles suspensions initially dispersed in water. Scale bar is 20 µm.  The background texture was an artefact of the microscope used.

Figure S4.  Impact of GIT region on the mean particle diameter (d32) determined by static light scattering of samples containing TiO2 particles initially dispersed in water: NPs = nanoparticles; FPs = fine particles.  Bars designated with different capital letters (A, B, C, D) were significantly different (Duncan, p < 0.05) when compared between different GIT regions (same sample). Bars designated with asterisks (*) were significantly different (Duncan, p < 0.05) when compared between different samples in the same GIT region.

Figure S5.  Impact of GIT region on the -potential of TiO2 particles: NPs = nanoparticles; FPs = fine particles.  Bars designated with different capital letters (A, B, C, D) were significantly different (Duncan, p < 0.05) when compared between different GIT regions (same sample). Bars designated with asterisks (*) were significantly different (Duncan, p < 0.05) when compared between different samples in the same GIT region.

Figure S6.  Influence of solution pH on the mean particle diameter (d32) of aqueous suspensions of TiO2 particles: NPs = nanoparticles; FPs = fine particles.

Figure S7.  Impact of pH on the -potential of TiO2 particles suspended in aqueous solutions: NPs = nanoparticles; FPs = fine particles.

Figure S8.  Impact of GIT region on the particle size distribution of emulsions in the absence and presence of TiO2 particles: NPs = nanoparticles; FPs = fine particles.

# Table S1. Chemical composition of simulated GIT fluids used to prepare the mouth, stomach and small intestine phases of the gastrointestinal tract model.

| Digestion Phase | Compound | Amount |
| --- | --- | --- |
| Mouth Phase | Sodium chloride | 13.64 mM |
|  | Ammonium nitrate | 2.05 mM |
|  | Monopotassium phosphate | 2.34 mM |
|  | Potassium chloride | 1.35 mM |
|  | Potassium citrate | 0.50 mM |
|  | Uric acid sodium salt | 0.06 mM |
|  | Urea | 1.65 mM |
|  | Lactic acid sodium salt | 0.65 mM |
|  | Porcine gastric mucin (type II) | 15 mg/mL |
| Stomach Phase | Sodium chloride | 17.11 mM |
|  | Hydrochloric acid | 41.91 mM |
|  | Pepsin | 1.6 mg/mL |
| Small Intestine Phase | Calcium Chloride Dihydrate | 10 mM |
|  | Sodium Chloride | 150 mM |
|  | Bile Salts | 5 mg/mL |
|  | Lipase | 1.6 mg/mL |